XMM Optical Monitor

MULLARD SPACE SCIENCE LABORATORY

UNIVERSITY COLLEGE LONDON	Author: Nigel R Bray

MSSL  XMMOM

DOCUMENT:

Distribution:

| XMM-OM Project Office | R Hunt | ü |
| --- | --- | --- |
| ESA PX | H Eggel |  |
| CSL | P Rochus |  |
|  | S. Roose |  |
| Los Alamos | C Ho |  |
| Royal Greenwich Observatory | R Bingham | ü |
| University College London | J Fordham | ü |
| Mullard Space Science Laboratory | N Bray |  |
|  | R Card |  |
|  | M de la Nougerede |  |
|  | R Chaudery |  |
|  | A Dibbens | ü |
|  | H Huckle |  |
|  | G Davison |  |
|  | T Kennedy |  |
|  | M Carter | ü |
|  | D Self |  |
|  | P Smith |  |
|  | P Thomas |  |
|  | H Kawakami | ü |
|  | M Whillock |  |
|  | K Mason |  |
|  | A Smith | ü |

| Author: | Nigel R Bray | Date: |  |
| --- | --- | --- | --- |
| OM Project Office |  | Date: |  |
| Distributed: |  | Date: |  |

Material SFO 32 AS

Fibre Size 8mm at large end

Magnification 3.37:1

Quality Area 25mm diameter minimum at large end

Quality Zones as per CCD quality specification attached

Mechanical Dimensions as per drawing and table below

Finishes:	Surface i. optically polished to £4 fringes flat
Surface ii. optically polished to £17 fringes flat
Surfaces iii. And corner radiuses R1, R2, R3, R4 to be bright polished

Parallelism: Surfaces i. and iv. to be parallel within 0.05mm

Distortion: Shear £50mm at large end
Gross - best fit of a straight line across the useful area <2%
Pincushion / Barrel <3%
Image run-out <200mm

Note: Dimension F is larger than the active area.  (To allow for optical bonding)

| Dimension | Value | Tolerance | Note |
| --- | --- | --- | --- |
| A | 2mm | MIN | straight section |
| B | 8.65mm | ±0.1mm |  |
| C | 23.5mm | ±0.1mm |  |
| D | 26.9mm / 26.85mm | MAX / MIN |  |
| E | 29.5 | ±0.1mm |  |
| F | 8.8 | MIN |  |
| R1 | 0.3 | +0, -2mm |  |
| R2 | 0.5 | ±0.1mm |  |
| R3 | 0.5 | ±0.1mm |  |
| R4 | 0.3 | ±0.1mm |  |

Table 1 : Mechanical Dimensions.

CCD QUALITY SPECIFICATION

(All measurements at the large end)

Zone 1	8mm	Centre dia

Zone 2	8mm to 15mm dia

Zone 3	15mm to 25mm dia

Blemish (Sports) measured at large end with diffused light and magnification.

Size	Zone 1	Zone 2	Zone 3

<25µ m	<0.5% of area	<0.5% of area	<0.5% of area

>25µ m <50µ m	3	6	7

>50µ m <75µ m	1	3	5

>75µ m	0	0	 0

Chickenwire (Line blemishes) measured at large end with diffused light and magnification.

Chickenwire <2 fibers wide use following table

Chickenwire >2 fibers wide treat as blemish (length + width) \ 2

Length of C-W		Incidences Allowed

Zone 1	<0.5mm			Disregard

>0.5mm <1.0mm		      1

>1.0mm			      0

Zone 2	<0.5mm			Disregard

>0.5mm <1.0mm	               	      6

>1.0mm <1.5mm		      4

>1.5mm			      0

Zone 3 	<1.0mm			Disregard

>1.0mm <2.0mm		      5

>2.0mm <3.0mm		      3

>3.0mm			      0

Required is the minimum necessary to ensure conductivity across surfaces assuming an ITO coating applied post manufacture.